## Slide 1
a)
b)
c)
Ba
Co
As
O
b
a
c
b
a
f)
O1
O2
d)
J1
J3
Co2+
Co2+
87.7°
O2-
+V
J1 superexchange (FM)
e)
+V
J3 third nearest-neighbor exchange (AFM)
g)
O2-
O2-
d3
d1
d2

## Slide 2
Co2+
Co2+
87.7°
O2-
+V
J1 superexchange (FM)
J3 third nearest neighbor exchange (AFM)
Co2+
Co2+
As5+
Co2+
Co2+
V5+
+V

## Slide 3
*
*
*
*
*
*
(003)
(006)
(009)
(2-10)
(0012)

## Slide 5: BaCo2(AsO4)2 (BCAO)
BaCo2(AsO4)2, or BCAO, has been one of the most intensely-studied Kitaev spin liquid candidates in recent years.
Believed to possess only weak Heisenberg and other non-Kitaev interactions.
  Largely owing to the slight trigonal distortion of the Co octahedra.
Interplanar AFM interactions are largely suppressed by the application of a weak (0.5 T) field, producing a nonmagnetic state.
92.3°
85.7°
Notes: Another material system for which existing synthetic methods have been rather limited, BaCo2(AsO4)2, has been one of the most intensely studied Kitaev spin liquid candidates of the past several years.
The honeycomb lattice in BaCo2(AsO4)2, or BCAO, consists of edge-sharing, lightly-distorted CoO6 octahedra, which are believed to account for the high degree of planar anisotropy observed in its magnetic behavior at low temperatures.
BCAO orders antiferromagnetically at TN = 5.4 K, with dominant antiferromagnetic interlayer coupling and in-plane ferromagnetic exchange, and has been shown to transition to a nonmagnetic state with the application of only a relatively weak field, suggesting the presence of fairly weak non-Kitaev interactions in the material.

## Slide 6: Substitutions
P
V
Sb
In order to reduce the degree of the trigonal distortion of the Co octahedra, various substitutions were attempted.
The most promising appears to be partial substitution of As with V.
  Correspond to a roughly 0.95 Å contraction and 0.01 Å expansion of the c-axis and a-axis, respectively.
Samples crystallize nicely from the melt, without a particular temperature gradient or cooling rate.
BaCo2(AsO4)2
Pb
Sr
[TO4]3- | T-O bond length
(PO4)3- | 1.50-1.60 Å
(AsO4)3- | 1.70 Å
(VO4)3- | 1.72 Å
(NbO4)3- | 1.82 Å
(SbO4)3- | 1.95 Å
b
a
Rep. BCAO-V-10% crystal

## Slide 7
BaCo2(AsO4)2
R-3
BaCo2(VO4)2
I41/acd
BaCo2(AsO4)>0.67(VO4)<1.33
R-3
Ba
As
Co
O
V
JKΓ/XXZ model
TN = 5.4 K
Strongly anisotropic magnetism (easy c-axis)
LRO suppressed by a 0.55 T field.
XXZ model
TN = 5.5 K
(1-D spin chain  3-D AF-LRO)
Strongly anisotropic magnetism (easy c-axis)
AFM order suppressed by a 3.9 T field (to incommensurate phase).
Faure, Q, et al, Nat. Phys., 14, 716-722 (2018)
Notes: Ba: 6-coord  12-coord

## Slide 8
Hysteresis
Metamagnetism
BaCo2(AsO4)2
BaCo2(VO4)2
b
a
c
c
b
a

## Slide 9
AFM
Order
Paramagnet
Spin glass
BaCo2(AsO4)2-2x(VO4)2x
Critical
point

## Slide 10
a)
b)

## Slide 11
pXRD (powder) – first heat
pXRD (crystal) – second heat/melt
SCXRD from the refinement assuming
no V (Max’s suggestion so far).

## Slide 12
pXRD (powder) – first heat
pXRD (crystal) – second heat/melt
SCXRD from the refinement assuming
no V (Max’s suggestion so far).

## Slide 13
a)
b)
θ
θ2
θ1

## Slide 14
From cifs derived from Rietveld refinements on second heat (melt) samples.
Large error bars of course, but seems to track roughly with gradual suppression of the order up to 7.5% V, more interesting behavior at 10-15% V, and gradually more glassiness/BCVO behavior.
  If the 10% trigonal distortion is actually smallest, that might make some sense?
  General trends, not correlated.
Likely won’t include - error bars from the refinements likely too large to get this info directly.

## Slide 15
a)
b)

## Slide 16
Notes: 4 A1g modes from oxygen, 1 A1g mode for Co/As respectively.

## Slide 17
x = 0.025
x = 0.05
x = 0.075
x = 0.10
x = 0.15
x = 0.20
BaCo2(AsO4)2-2x(VO4)2x
x = 0.15
(h k 0)
(h k 0)
(h k 0)
(h k 0)
(h k 0)
(h k 0)
[1 -1 0]
[-1 0 0]
[1 -1 0]
[-1 0 0]
[1 -1 0]
[-1 0 0]
[1 -1 0]
[-1 0 0]
[1 -1 0]
[-1 0 0]
[1 -1 0]
[-1 0 0]
a)
b)
c)
d)
e)
f)

## Slide 18
(x,x) singlet modes
Relative to the (x,y) polarization, only the Ag(6) mode follows a similar trend (shift to lower frequency, slight broadening).
The Ag(2) and Ag(3) modes are very weak, and are not visible at higher V concentrations.
For the Ag(1) and Ag(4) modes, the 10% V sample shows a sharper shift to higher frequency, with no significant broadening.

## Slide 19
(x,x) doublet modes
The 10.0% V sample shows all doublet modes at a higher frequency (a local maximum in terms of V-content).
These modes seem to generally agree with magnetization/specific heat measurements showing this composition to be at some critical point in the series.
The frequency shift of doublet modes beyond 10% sub. varies.
The Eg(2) mode shows significant broadening, while the Eg(3), Eg(4), and Eg(5) modes show a slower broadening.

## Slide 20
(x,y) singlet modes
The Ag(1), Ag(4), and Ag(5) modes both shift to lower energy and broaden upon increasing V-content.
The 10% V sample shows either a much sharper shift to lower frequencies, or no mode at all in the case of the Ag(2) and Ag(3).

## Slide 21
(x,y) doublet modes
The 10.0% V sample shows only the Eg(1) and Eg(2) (a local maximum in terms of V-content).
  The Eg(4) mode also isn’t visible for this sample.
The frequency shift of doublet modes beyond 10% sub. varies.
The Eg(1), Eg(2), and Eg(3) modes don’t broaden much, but the Eg(4), and Eg(5) modes broaden significantly above 10% V.
  At 10% V, these are also the narrowest or not present.

## Slide 22
a)
b)
c)
d)
e)
f)
g)
h)

## Slide 23
b)
a)

## Slide 24
a)
b)
c)
d)
e)
f)

## Slide 25
d)
e)
f)
a)
b)
c)

## Slide 26
a)
b)
0.025
0.05
0.075
0.10
0
0.15
d)
0.20
c)

## Slide 27
x↑
x↑

## Slide 28
x↑
x↑

## Slide 29
0
0
0
0
0
0
0
0
0
0
0
0

## Slide 30
0
0
0
0
0
0
0
0
0
0
0
0

## Slide 31
b)
c)
a)

## Slide 33
a)
b)
c)
d)
e)
f)

## Slide 34
f↑
f↑
f↑

## Slide 35
f↑
f↑

## Slide 36
a)
b)
c)
d)
e)
f)

## Slide 37
Composition (nom.) | Tf (300 Hz) (K) | Ea (K) | ω0 (Hz)
BCAO-10% V | 2.73 | 85.0 | 1.06 x 1016
BCAO-15% V | 2.63 | 53.7 | 2.16 x 1011
BCAO-20% V | 2.79 | 56.8 | 2.14 x 1011
Ea = average thermal activation energy;
ω0 = characteristic frequency
For conventional glassy systems, ω0 ≈ 1010- 1013
Cluster glasses closer to ω0 ≈ 1016

## Slide 39
x↑

## Slide 42
a)
b)
c)
d)
e)
f)

## Slide 43
a)
b)
d)
e)
c)
f)